## Slide 1: High-efficient and automatic determination of Hansen Solubility (dispersibility) parameters of micro-, nano-particles and quantum dots by instrumental in-situ visualization and quantification of sedimentation behavior under normal or high gravity. Dietmar Lerche, LUM GmbH, Berlin, Germany

## Slide 2: First of all: It´s not only me; it´s a team work Many thanks to: Sebastian Süß Wolfgang Peukert Doris Segets Institute of Particle Technology (LFG), FAU, Erlangen, Germany Titus Sobisch Luis Rodriguez Sonja Horvat LUM GmbH & Dr. Lerche KG, Berlin, Germany

## Slide 3: Introduction
3
Nano@microparticles are essential to innovative products.
A dispersion or formulation step into a liquid phase is often mandatory.
The liquid/continuous phase must suite the specific requirements, dispersed state of particles should not change over product life time.
Particle and its surrounding liquid have to be adjusted to each other

## Slide 4: Relevant particles characteristics for dispersion
4
A. Geometrical characteristics
Size, Size Distribution, Shape
B. Surface characteristics
Surface morphology, chemical composition, ions, surfactance, coating materials (e.g. polymers), pickering particles
Hansen Solubility Parameter
since 50 years

## Slide 5
How to determine the HSP of particles?
Experimental task:
1. to choose a set of test liquids covering more
or less the 3D-Hansen space (or interested part)
2. to disperse particles into different test liquids
3. to „detect“ the behavior „How suspensed do they stay“
4. to score the observation from 0 to 1
5. to calculate HSP (e.g. HSPiP Software package)

## Slide 6
2. Ranking of liquids: Good or Bad
1. Quantification of particle behavior in liquids/continous phases
M. Bixenman et al. (2010) Quality control of cleaniless of electronic parts
Why does not everyone use the HSP approach?
C. Hansen introduced quantification as a merit of sedimentation time or velocity
subjective
time consuming for nano
3. No standardized routine method.

## Slide 7
How to determine the HSP of particles?
Experimental task:
1. to choose a set of test liquids covering more
or less the 3D-Hansen space (or interested part)
2. to disperse particles into different test liquids
3. to instrumentally „detect“ the behavior
4. to automatically score the observation from 0 to 1
5. to calculate HSP (e.g. HSPiP Software package)

## Slide 8
In-situ visualization of dispersion state
by STEP-Technology
NIR
VL
X-Ray
12 channels,
l = 870, 470 nm
t1 > t0
Conventional
“one point” techniques
Space and Time resolved
Extinction Profiles
Animation see:
Youtube channel ‚LUM GmbH‘
Notes: Aimation in der Mitte anhalten

## Slide 9
In-situ visualization of particle sedimentation
- lg = Et,p = e . ct,p . d
Extinction/Concentration:
Tt,p =
Transmission:
It,p
I0
It,p
I0
start
last profile
start
last profile
Meniscus
Meniscus
Bottom
Bottom
LUMiSizer experiments. Visualization and analysis by Software Package SEPView
Notes: Iolitec 0.05%

## Slide 10
General SOP:
1. Select appropriate continuous phase/liquid
HSPs available from HSPiP
List of liquids used for Finn Talc 15
Liquid

## Slide 11
General SOP:
2. Disperse particles into continuous phases,
measure sedimentation at earth or higher gravity
of up to 12 samples simultaneously.
LUMiSizer:
Time Interval:
2s to hours 10s
Temperatur:
4 to 25°C
Acceleration
6 to 2300
times earth
gravity
N-Methylformamide
Methanol
Isopropanol
n-Heptane

## Slide 12
General SOP:
3. Calculate sedimentation time (ST) based on Integral Extinction (IE)
Sedimentation time
E0 = extinction of
pure liquid
ST = time to
reach
E0 + 0.15
(or any
appropriate value
according to
sedimentation kinetics)

## Slide 13
Absolute ST of Finn Calc dispersed in different liquids
General SOP:
3. Calculate sedimentation time (ST) based on
Integral Extinction (IE)

## Slide 14
General SOP:
4. Relative sedimentation times RST
Proposed by C. Hansen
Extention for dimensionless RST
Accounts also for gravity
and optical path
liquids
Accounts for density &
viscosity differences

## Slide 15
15
Finn Talc M15
δd =12.1 MPa0.5; δP =17.7 MPa0.5
δh =3.9 MPa0.5; R0 =9.1 MPa0.5
by HSPiP-software, Abbott
Lerche et al., Dispersion Letters 5 (2015) 13 - 18
Süss et al., in preparation
Normalization of RST
General SOP:
5. Score RST to 0, 1
6. Calculate HSPs
Score by rounding
Notes: Good, bad????

## Slide 16
Liquid | purity / % | purpose | company
1. n-hexane (Hex) | ≥ 95 | screening | C.Roth, Germany
2. triethylamine (TEA) | ≥ 99.5 | screening | C.Roth, Germany
3. p‑xylene (Xyl) | 99 | screening | Sigma-Aldrich, Germany
4. N-methyl-2-pyrrolidone (NMP) | ≥ 99.8 | screening | C.Roth, Germany
5. 1.4-dioxane (Diox) | ≥ 99.5 | screening | C.Roth, Germany
6. ethyl acetate (EA) | > 99.5 | screening | C.Roth, Germany
7. tetrahydrofuran (THF) | ≥ 99.5 | screening | C.Roth, Germany
8. isopropyl alcohol (IPA) | ≥ 99.8 | screening | C.Roth, Germany
9. acetonitrile (ACN) | ≥ 99.5 | screening | C.Roth, Germany
10. N,N-dimethylformamide (DMF) | ≥ 99.5 | screening | C.Roth, Germany
11. dimethyl sulfoxide (DMSO) | ≥ 99.5 | screening | C.Roth, Germany
12. methanol (MeOH) | ≥ 99.9 | screening | C.Roth, Germany
13. 2-butoxyethanol acetate (BAc) | ≥ 98 | screening | Merck, Germany
14. acetone (Act) | ≥ 99.8 | screening | C.Roth, Germany
15. n-pentane (Pent) | ≥ 99 | validation | C.Roth, Germany
16. methyl acetate (MA) | ≥ 99 | validation | C.Roth, Germany
17. dimethyl carbonate (DMC) | ≥ 99.8 | validation | C.Roth, Germany
18. 1.4-butanediol (BD) | ≥ 99 | validation | C.Roth, Germany
List of liquids used for CB study
Application Carbon Black

## Slide 17: HSP of Carbon black: Integral extinction in different liquids
Integral Extinction (IE) calculated of a ROI of 15 mm below meniscus
Region of IE to
determine RST.
must include
best and
worst solvent.

## Slide 18: HSPs of Carbon Black Comparison of Printex® L & Printex® U
HSP in same range, but different due to manufacturing process
Developed approach sensitive to distinguish both products
 | δD / MPa0.5 | δP / MPa0.5 | δH / MPa0.5 | R / MPa0.5
Printex® L | 16.56 | 9.5 | 9.42 | 5
Printex® U | 17.35 | 8.22 | 7.29 | 4.3
Score by
rounding

## Slide 19
Processing (energy, time) alters
surface properties of CB
15 min sonic bath
1
2
3
HSP
0
5
10
15
D
P
H
1 min sonotrode
1
2
3
0
5
10
15
D
P
H
10 min sonotrode
1
2
3
0
5
10
15
D
P
H
HSP
HSP
Stock concentration of Carbon Black 0.7 g/l,
A: 1. 15 sec Vortex + 15 min US bath, 2. diluted to 0.014 g/l, 3. again 15 min US bath
B: 1. 15 sec Vortex + 5 min US bath, 2. diluted to 0.014 g/l, 3. 1 min US treatment
C: 1. 15 sec Vortex + 5 min US bath, 2. diluted to 0.014 g/l, 3. 10 min US treatment
US treatment: 3 – 4 ml Suspension, IKASONIC U 50, Amplitude 100 %, Cycle 1, Sonotrode 600 W/cm²
Score by
rounding
Notes: eventuell 1 min rausnehmen?

## Slide 20
HSP of Carbon black (HSPiP)
(C. Hansen)

## Slide 21
Validation of HSP regarding chosen IE and CA
for RST determination

## Slide 22: Validation of HSP approach by dispersing into a “good” liquid
Printex® L dispersed
into Diethylene
Glycol Butylether
Expected based on
Liquid HSPs
to be “good”
Solvent is ranked as good solvent

## Slide 23: Validation of HSP approach by mixing “good” and “bad” liquids
Tailoring continuous phases regarding dispersibility
100% Ethylacetat
100% 1.4-Dioxane

## Slide 24: Validation by targeted surface decoration of ZnO quantum dots
Synthesis of QD: Acetate molecules on ZnO surface
ZnAc + LiOH
Ligand exchange: Catechol (CAT) molecules on ZnO surface
Dispersing procedure for ZnO
- preparation of 0.1 wt.-% ZnO dispersion in different solvents
15 minutes sonication (30 W)
solvents: n-hexane, Toluene, NMP, 1.4-Dioxane, Ethyl acetate, Acetone, Diacetone alcohol, THF, IPA, DMSO, Propylene-1,2-carbonate, MeOH, H2O, EtOH
Coordinated acetate
Reduction of polar
contribution by
larger carbon content
+ benzene ring
Increase of
disperse contribution by carbon backbone

## Slide 25
Decreased δP for ZnO+CAT1 as expected
 | δD / MPa0.5 | δP / MPa0.5 | δH / MPa0.5 | R / MPa0.5
ZnO 20h 2ML | 15.46 | 23.31 | 15.45 | 15.4
ZnO + Cat1 20h 2ML | 14.61 | 3.17 | 14.51 | 7.9
ZnO + Cat2 20h 2ML | 21.05 | 7.9 | 15.09 | 11.2
Increased δD for ZnO+CAT2 as expected
ZnO quantum dots (QD): Influence of surface molecules
Score by
rounding

## Slide 26
Summary I
1. Sedimentometer equipped with STEP-Technology allows for instrumental in-situ visualization and quantification of particle settling behavior in different liquids.
2. High flexibility due to different wavelengths, light factors, acceleration factors and optical path of sample cells.
3. HTP due to centrifugal acceleration and multisample approach (n = 12).
4. Determination of experimental sedimentation time (STi) based on integral extinction (SEPView).
5. Calculation of the dimensionless relative sedimentation time (RSTi) and normalization by RSTi/RSTmax

## Slide 27
Summary II
6. Automatic scoring:
a) Scoring simply by rounding RSTnorm (< 0.5 good, > 0.5 bad)
(treshold has to be changed to have at least 2, better 3 continuous phases in each score, or use additional liquids)
b) Automatic determination of number of good liquids by determining the minimum of change of the distance of HSP sphere adding consecutively another liquid „ranked“ as good.
7. Entering the automatically good – bad liquids into HSPiP-Software and calculate HSPs by HSPiP-Software
8. Applicability of the instrumental and automatic scoring shown for pigments, Carbon Black and ZnO-QD and validation by mixing good and bad liquids or surface alterations.
9. Attention: HSPs may be altered by dispersion process (type, energy, time). Stay close to the real processing.

## Slide 28
Proposal to discuss:
HSP traditional Hansen Solubility Parameter
In case of particles engineers and scientists
are mostly interested in particle dispersibility,
not so much in particle solubility.
To avoid confusion, would it be better to call the parameters
HDP Hansen Dispersibility Parameters ?

## Slide 29
Thank you for your attention!!!
Questions??
More Information: See our booth (Adaptive Systems)
D.Lerche@LUM-GmbH.de, Colin@adaptive.com
www.LUM-GmbH.com,
www.Dispersion-Letters.com
Thanks to Prof. Abbott
for HSPiP and help
Thanks to S. van Loon
for Finn Calc M15
Thanks for funding: