## Slide 1: HANSEN SOLUBILITY PARAMETERS FROM START TO 50 YEARS
CHARLES M. HANSEN

## Slide 2: START WAS A PhD PROJECT (1962-1964) ”WHY IS SOLVENT RETAINED IN COATINGS?”
Hydrogen bonding was thought to be the cause of solvent being found in coatings after many years. The PhD project was carried out in a small industrial coatings research laboratory cooperating with the Technical University of Denmark.
HSP is a spin-off from this project.
Hydrogen bonding needed to be studied to show it had no effect on solvent retention. The retention is controlled by concentration dependent solvent diffusion with very, very slow diffusion near the air surface where there is essentially no solvent.

## Slide 3: Thermodynamic Equations
Berthelot (1898 - interaction between two unlike species - Geometric Mean)
ε12 = (ε11ε22)½
Scatchard (1931 - Exchange Energy, A12 , for mixing pairs of “1” and “2”)
A12 = (ε11 + ε22 - 2 ε12)
A12 = (ε11½ - ε22½)2
Hildebrand and Scott (1950/1964, 1962 - Regular Solution Theory )
ε Taken as Cohesion Energy Density
ε11 = ΔE1/V1; ε22 = ΔE2/V2
Definition of Hildebrand Solubility Parameter
δ = (ΔE/V) ½
Heat of Mixing
ΔEM ~ ΔHM = φ1φ2(x1V1 + x2V2)(δ1 - δ2)2
No Hydrogen or Polar Bonding, No Orientation

## Slide 4: BLANKS and PRAUSNITZ (1964)
THE HILDEBRAND TOTAL SOLUBILITY PARAMETER WAS DIVIDED INTO A DISPERSION PART (D) AND A ”POLAR” PART (A) WHILE KEEPING THE SAME TOTAL COHESIVE ENERGY. HYDROGEN BONDING STILL EXCLUDED – ALCOHOLS AND GLYCOLS WERE NOT INCLUDED.
δT2 = δD2 + δA2
CALCULATE FOR ALCOHOLS AND GLYCOLS

## Slide 5: δA VERSUS δD SOLUBILITY PLOTS SHOWED NEED FOR NEW ”DIMENSION”
Urea-formaldehyde “1001” δD δA
2-Ethyl hexanol YES NO 7.78 6.03
Cyclohexanol YES NO 8.50 6.93
1-Pentanol YES NO 7.81 7.17
1-Butanol YES NO 7.81 8.20
Acetone NO YES 7.58 6.13
Nitroethane NO YES 8.11 7.57
Acetonitrile NO YES 7.90 8.79
Gamma-Butyrolactone NO YES 9.26 8.82
Can calculate δD
Now divide δA into δP and δH
But How?
δA2 = δP2 + δH2

## Slide 6: CALCULATING D
HOMOMORPH CONCEPT (ED = E FOR SIMILAR HYDROCARBON)
CORRESPONDING STATE THEORY (CST)
CST FIGURE FOR ED FOR EACH OF ALIPHATIC, CYCLOALIPHATIC, OR AROMATIC STRUCTURE
ED versus V for Tr=T298.15./TCRITICAL

## Slide 7: FIGURE FOR ED FOR ALIPHATIC HYDROCARBONS

## Slide 8: INITIAL ATTEMPT TO ASSIGN P AND H TRIAL AND ERROR (1965-)
METAL BARS, MAGNETS, AND BEADS

## Slide 9: P - Final Result Adjusted from Trial and Error Values
Böttcher Equation, cal/cm3
When constants not available Beerbower Equation, MPa½
P = 37.4(µ)/V½
Later Functional Group Contributions

## Slide 10: H – Final Result (What was left over)
  EH = E - ED - EP
  H = (EH/V)½
  CHECK where possible that:
T2 = 2D + 2P + 2H
  Later Functional Group Contributions for EH

## Slide 11: P VERSUS H PLOT

## Slide 12: WHOLE EQUALS SUM OF PARTS E = COHESION ENERGY = ΔEvap
E = ED + EP + EH
D - Dispersion (Hydrocarbon)
P - Polar (Dipolar)
H - Hydrogen Bonds (Electron Interchange)
E/V = ED/V + EP/V + EH/V
  T2 = D2 + P2 + H2
  THREE DIMENSIONAL SOLUBILITY PARAMETER (1967)
  HANSEN SOLUBILITY PARAMETERS BEERBOWER (1970)
  T = Square Root of Cohesion Energy Density (Hildebrand) 88 in 1967; 243 in 1971,1200+ in 2007; 10,000+ Now

## Slide 13: ALAN BEERBOWER FIRST TO USE ”HANSEN”
Beerbower (1970) in ESSO brochure:
”The Hansen Principle”
“The energy of vaporization measures all of the forces that work to hold a liquid together; therefore, all interactions, regardless of whether they are dispersion, polar, or hydrogen bonding, or other types, are included in ΔE. Since δ is defined in terms of ΔE, all of the interactions are included in δ.”

## Slide 14: KEY HSP EQUATIONS
Ra2 = 4(D1 - D2)2 + (P1 - P2)2 + (H1 - H2)2
Ra is a distance in HSP space.The ”4” is experimentally verified giving spheres of radius Ro, rather than spheroids, and is found (approximately) in the new Yamamoto theory
RED = Ra/Ro
Relative Energy Difference is Distance to sphere center divided by its radius, Ro.
(RED)2 = (Ra/Ro)2 corresponds to 12 / c in Huggins/Flory Theory

## Slide 15: HSP AND SURFACE PHENOMENA EXAMPLES - FILMS, PIGMENTS, NANOPARTICLES
EPOXY FILM
A: Spontaneous spreading of droplets
(Zisman Critical Surface
Tension at Boundary)
B: No dewetting – Films are retained, droplets remain
C: Dewetting of Films
(ASTM Wetting Tension
At Boundary)

## Slide 16: CONTROL OF PROCESSES SELF-ASSEMBLY IN THIXOTROPIC PAINT
VERSAMID SEGMENTS ASSOCIATE IN HYDROCARBON SOLVENT
ALCOHOLS WILL DESTROY EFFECT
SHEAR BREAKS STRUCTURE TEMPORARILY

## Slide 17: SELF-ASSEMBLY IN WOOD HEMICELLULOSE SIDE CHAINS ORIENT
BOUNDARY HSP MATCH
(LIGNIN) (LIGNIN)
Ac Ac Ac Ac
2 3 2 3
M14M14M14G14M14G14M14M14G–
3 6
  1 1 M Ga
(CELLULOSE) (CELLULOSE)
GOOD HSP MATCH

## Slide 18: HSP FOR WATER
D P H Ro
Single molecule 15.5 16.0 42.3 —
>1% soluble in 15.1 20.4 16.5 18.1 Data Fit 0.856
Good/Total 88/167
Total miscibility 18.1 17.1 16.9 13.0
Data Fit 0.880
Good/Total 47/166

## Slide 19: HSP, HSPiP, AND THE “ANOMALIES” OF DIFFUSION
Solvent absorption different from straight line with square root of time is considered by most to be an “anomaly” (S-curves, straight line with linear time). Solutions to the diffusion equation using the HSPiP package confirm that these “anomalies” are caused by a delay or entry resistance at the surface. The surface entry coefficient increases with greater equilibrium solvent absorption (ΔHSP~0). Low equilibrium solvent absorption means fewer suitable sites for entry and increasing problems with adsorption.

## Slide 20: Coefficient for Surface Mass Transfer, h, Depends On Equilibrium Absorption. (COC, Topas® 6013) Equilibrium Absorption (Permeation) depends on ΔHSP
Chart: Correlation of log(h) with C
| 0.35100000000000031 | 0.26800000000000002 | 0.18100000000000024 | 0.17600000000000021 | 7.6000000000000123E-2 | 0.67600000000001204
 | -5.109 | -5.9172 | -6.8268 | -6.9281 | -7.8357 | -3

## Slide 21: SUMMARY
HSP have existed since 1967
Uses: Solubility (Gases, Liquids, Polymers, Solids),
Compatibility, Swelling, Chemical Protective Clothing,
Cosmetics, Controlled Drug Release, Barrier Films,
Packaging, API, Environmental Stress Cracking, Paint,
Self-Assembly, Physical Properties, Conservation of
Paintings, Surfaces, Nanoparticles, Improvement of
Physical Adhesion, Bitumen, Asphalt, Organic Salts,
Biological Materials, DNA, Zero-Release Flexo Inks .....
HSPiP: A primary source to interpret HSP phenomena.

## Slide 22: THANKS!
Heartfelt thanks to
Prof. Steven Abbott and to Dr. Hiroshi Yamamoto.
Without them the HSPiP would not exist as it does, nor would there have been the magnificent progress seen over the past 9 years. It is clear that this effort will continue in the future, and that a conference such as this one and contacts with HSPiP users will stimulate future developments. Thanks, as well, to our excellent hosts at the University of York.
I am happy to have lived to see what has happened with my early studies. I am now sure that the HSP methodology will survive in some form. I hope the 50th Anniversary HSP Conference will be as memorable for each of you as it will be for me.